## Slide 1: Metallurgical aspects of the ET beampipe design
FWO workshop | Alexey Gervasyev | 27 November 2023
Department of Electromechanical, Systems and Metal Engineering
  Materials Science and Technology group

## Slide 2
Outline
General ET beampipe design considerations
Overview of steels potentially to be used as the beampipe material
Ferritic stainless steel welded joint formability

## Slide 3
General ET beampipe design considerations
Pipe making technology:
Spiral welded
Longitudinally welded
Double longitudinally welded
Already 27 combinations, but there are other aspects…
Reinforcement:
Stiffener rings
Corrugations
No reinforcement
Material:
Austenitic stainless steel
Ferritic stainless steel
Non-stainless low-carbon steel
NEW
120 km long, 1 m diameter ultra-high vacuum pipeline
3 (sub-size) pre-prototypes made of the 3 materials
50 m pilot sector
To be produced at CERN

## Slide 4
[Aniello Grado, Beampipes for Gravitational Wave Telescopes seminar at CERN, March 2023]
General ET beampipe design considerations

## Slide 5
[CERN]
General ET beampipe design considerations

## Slide 6
[muelheim-pipecoatings.com]
Overview of steels potentially to be used as the beampipe material
Commercially available line pipes

## Slide 7
[mannesmann-grossrohr.com]
Commercially available line pipe – product range
Overview of steels potentially to be used as the beampipe material

## Slide 8: Overview of steels potentially to be used as the beampipe material
[Rajasekhara et al 2011]
[WorldAutoSteel]
Steel can be very different

## Slide 9: Overview of steels potentially to be used as the beampipe material
[Gervasyev at al]
Steel microstructure complexity

## Slide 10: Overview of steels potentially to be used as the beampipe material
Stainless
Chart: Price (Euro/kg)
| 316L | 304L | 444 | 430 | 1010 | A36 | HSLA HR YS550 | DP HR YS400 | DP CR YS600 | IF CR YS260
Price (Euro/kg) | 3.86 | 3.135 | 1.815 | 1.335 | 0.794 | 0.817 | 0.7935 | 0.8345 | 0.8415 | 0.8225


Non-Stainless

## Slide 11: Overview of steels potentially to be used as the beampipe material
Stainless
Chart: Price (Euro/kg)
| 316L | 304L | 444 | 430 | 1010 | A36 | HSLA HR YS550 | DP HR YS400 | DP CR YS600 | IF CR YS260
Price (Euro/kg) | 3.86 | 3.135 | 1.815 | 1.335 | 0.794 | 0.817 | 0.7935 | 0.8345 | 0.8415 | 0.8225


Specific absorbed energy (J/cm3) | 212.75 | 284.625 | 168 | 126.55 | 141.7 | 103.25 | 123.4 | 131.48 | 142.5 | 162.6
Non-Stainless

## Slide 12: Overview of steels potentially to be used as the beampipe material
Chart: Price (Euro/kg)
| 316L | 304L | 444 | 430 | 1010 | A36 | HSLA HR YS550 | DP HR YS400 | DP CR YS600 | IF CR YS260
Price (Euro/kg) | 3.86 | 3.135 | 1.815 | 1.335 | 0.794 | 0.817 | 0.7935 | 0.8345 | 0.8415 | 0.8225


Yield strength (MPa) | 240 | 205 | 312.5 | 295 | 243.5 | 271 | 600 | 395 | 675 | 290
Stainless
Non-Stainless

## Slide 13: Overview of steels potentially to be used as the beampipe material
Chart: Price (Euro/kg)
| 316L | 304L | 444 | 430 | 1010 | A36 | HSLA HR YS550 | DP HR YS400 | DP CR YS600 | IF CR YS260
Price (Euro/kg) | 3.86 | 3.135 | 1.815 | 1.335 | 0.794 | 0.817 | 0.7935 | 0.8345 | 0.8415 | 0.8225


Stainless
Non-Stainless
Excellent
Good
Not-so-good

## Slide 14: Overview of steels potentially to be used as the beampipe material
Chart: Pipeline wall thickness (mm)
LIGO per meter | 264
Line pipes | 42.48 | 42.396 | 47.1336 | 47.76 | 51.8664 | 52.56 | 56.5896 | 59.52
Pipe manufacturing and pipeline construction
Pipe manufacturing and pipeline construction??
Pipeline construction??

## Slide 15
Austenitic stainless steel alternatives (to reduce the cost)
Ferritic stainless steel
Non-stainless steel
Formability of welded joints?
Cleaning?
Overview of steels potentially to be used as the beampipe material

## Slide 16
Ferritic stainless steel welded joint formability
The immediate task is to produce pre-prototypes of the ET beam pipe, smaller diameter pipe sections to be manufactured in CERN
The pre-prototypes are longitudinally welded corrugated pipes, corrugations are applied by cold forming of the welded pipe
AISI 430 FSS welds failed by brittle cracking during the cold forming
Grades 444 and 441 demonstrated better performance but some damage still occurred
Change of the welding process from TIG to laser welding apparently led to satisfactory results
Metallurgical aspects of the FSS welding in these challenging conditions must be understood

## Slide 17: Base metal
430
444
441
800μm
800μm
800μm
ND
RD

## Slide 18: Base metal
430
444
441
200μm
ND
RD
200μm
200μm
Ti Kα
Nb Kα
Cr Kα

## Slide 19: 430 TIG welding joint
1 mm

## Slide 20: 444 TIG welding joint
1.5 mm

## Slide 21: 441 TIG welding joint
1.5 mm

## Slide 22: 444 Laser (pulsed) welding joint
1.5 mm

## Slide 23
Tungsten Inert Gas (TIG) welding parameters
(aka Gas Tungsten Arc Welding (GTAW), an arc welding process that produces the weld with a non-consumable tungsten electrode)
Pulsed
I =40 A to 85 A
Pulse time = 0,15 s
V = 12 V
Speed = 130…145 mm/min
=> Heat input ≈ 185 J/mm
Basic welding heat transfer model

## Slide 24: Basic welding heat transfer model
T | Temperature | 
T0 | Initial temperature | 
t | Time | 
Q | Heat input | 180000
d | Thickness | 0.0015
ρ | Density | 7800
λ | Mean thermal conductivity | 25
c | Mean specific heat capacity | 420
α | Mean heat transfer coefficient | 180
r | Distance between the heat source and the modelled point | 0.00613
T |  | 
T0 |  | 
t |  | 
Q |  | 180000
d |  | 0.0015
ρ |  | 7800
λ |  | 25
c |  | 420
α |  | 180
r |  | 0.00613
With the peak temperature of 1350°C
[N.N. Rykalin (1951)]

## Slide 25: Basic welding heat transfer model
Chart: Time (s)
Chart: Distance from the heat source (mm)
Chart: Time (s)
Chart: Cooling speed (°C/s)
180 kJ/m – heat input estimated from the welding parameters, 240 and 120 kJ/m – arbitrary higher and lower heat inputs

## Slide 26: Dilatometer simulations
TD
RD
Thermocouple welding spot
Microstructure measurements
Dilatometer specimen:
10 mm × 5 mm ×
sheet thickness (1.5 mm)
Dilatometer measures dimensional changes in material as a function of temperature.
It can implement complex temperature-time programs with high heating and cooling rates using induction heating and cooling by inert gas stream.

## Slide 27: Dilatometer simulations
Two treatments: much faster and much slower cooling rates compared to the model estimation
Chart: Time (s)
Chart: Time (s)
Chart: Cooling speed (°C/s)

## Slide 28: 444 Dilatometer simulations
Fast dilatometer treatment
Slow dilatometer treatment
ND
RD
1.5 mm
1.5 mm

## Slide 29: 444 Dilatometer simulations
Fast dilatometer treatment
Slow dilatometer treatment
200μm
200μm

## Slide 30: 444 Dilatometer simulations
Fast dilatometer treatment
Slow dilatometer treatment

## Slide 31: 444 Dilatometer simulations
Fast dilatometer treatment
Lazer welding HAZ
200μm
200μm

## Slide 32: 444 Dilatometer simulations
Slow dilatometer treatment
TIG welding HAZ
200μm
200μm

## Slide 33
Corrugated 444 TIG weld with failure
Since the fracture is (quasi-)brittle, there are secondary cracks which can be used to analyse the fracture characteristics.
Therefore, electropolishing was used to prepare the sample (it doesn’t blunt the edges of the secondary cracks too much).
400 µm

## Slide 34
Corrugated 444 TIG weld with failure
Intragranular fracture corresponds to the {001} cleavage planes (cube face)
Intergranular fracture is also present
(?)
(?)
(?)

## Slide 35
Corrugated 444 TIG weld with failure
(Deformation) twinning detected
Σ3 CSL boundaries

## Slide 36
Corrugated 444 TIG weld with failure
Strain heterogeneities (shear/deformation bands, twins) formed during the cold forming in combination with the grain boundary precipitation could provide conditions for cleavage fracture initiation.
Cleavage fracture propagation is then easy due to the large grain size.
1250 µm
KAM (°)

## Slide 37
Unlike grade 430, grades 444 and 441 never transform to austenite
The microstructure of 444 and 441 steels is therefore defined by the ferrite grain size and Nb and Ti –based precipitation which occurs both inside ferrite grains and along their boundaries
It doesn’t appear feasible to completely supress the grain boundary precipitation by quenching
Therefore, the only way to improve the weld toughness (given any post-heat-treatment is not practical) is to reduce the grain size (which was to a significant extent achieved by laser welding).
Finer grain size should
  Improve the resistance to cleavage fracture propagation,
  Reduce the propensity to form strain heterogeneities.
Comments – FSS weld formability

## Slide 38
Collaboration between the Materials Science and Technology group of UGent and the Materials sector of CERN has been established
The work so far has been focused on the welding technology optimization to allow the manufacturing of the ferritic stainless steel pre-prototype
The results suggest that the use of very low heat input welding technique (laser) and stabilized FSS grades 444 or 441 allows to achieve good enough formability of the welds to withstand the corrugation forming process, and therefore the FSS pre-prototype can be manufactured identically to the other two
That said, if the FSS becomes the material of choice, corrugation should probably be avoided (and stiffener rings should be used instead)
Another important activity is to search for and to work with industrial partners who are to help with the pilot sector manufacturing
Concluding Comments

## Slide 39
Thank you!

## Slide 40: Alexey Gervasyev Post-doctoral researcher Materials Science and Technology group alexey.gervasyev@ugent.be www.ugent.be
Universiteit Gent @ugent
@ugent Ghent University