## Slide 1: The ET beampipe vacuum system
Nick van Remortel
University of Antwerp, Belgium
IRI Workshop
November 27, 2023

## Slide 2: Residual gas noise contribution for ET:
Source: ET design report update 2020
Impact of residual gas in ET’s optical beam:
Affect phase of laser field as gas molecules transverse the beam, proportional to:
  mass,
  square of polarizability
  Partial pressures
Noise on mirrors as gas particles collide with mirror surface: gas damping at low f
Mirror cleanliness
Acoustic isolation
Source: S.E. Whitecomb, LIGO-T840003

## Slide 3: Pressure impact on power spectral density noise curve
Source: M. Zucker and S. E. Whitcomb, LIGO DCC P940008
Impact on power spectral density:
Density ~partial pressure
Simple calculation assumes constant pressure profile
Pressure profile depends on:
  Outgassing rate, Q
  Pump distance, L
  Pumping speed, S
  Pipe conductance, C

## Slide 4: Scattered light
Optical aperture of ET’s laser beam
Minimal aperture of vacuum tube design with constant radius determined by the losses close to the mirrors
Aim to maintain losses below Lc<10-8 implies rpipe=0.42m (HF) rpipe=0.31m (HF)
source: M. Andrés-Carcasona et al. arXiv:2307.14104 [gr-qc]
Notes on pipe diameter:
Has impact on tunnel diameter
Tunnel excavation price scales with diameter
Current tunnel diameter: 6.5m
Optical baffles shield mirrors from stray light
Typical baffle size is 0.1 m
Implies minimal beam pipe diameter of 1m
If pipe needs bakeout: thickness of insulation
Welding/repair and safety margins

## Slide 5: Baffles
source: M. Andrés-Carcasona et al. arXiv:2307.14104 [gr-qc]
Analogous to aLIGO and adV the vacuum system will be equipped with conical baffles shielding the aperture from stray light due to mirror finite aperture and aberrations
Baffles in ET will start at end of the cryotraps connected to the mirror vacuum towers
Position of first baffle: 32m (HF), 72m (LF)
Recursive formula for distances of other baffles
W= farthest point form which photons should be shielded
Distance between baffles increases rapidly with distance from the main mirrors
Beampipe radius
Mirror radius
Nr of baffles needed for various pipe diameters,
Assuming unequal (minimum) or equal spacing
Default configuration for simulations

## Slide 6: Scattered light simulation
Contains many ingredients:
Mirror surface quality impacts BRDF
Longitudinal vibration of baffles induce phase shifts
Various sources of noise & mitigation:
  Diffraction: serrate edges of baffles
  Backscattering
  Reflection on edges: serrating
  Shining surfaces: do not expose beam pipe to photons

## Slide 7: Effect of dust
Source: A. Moscatello at 2nd ET annual meeting, Orsay, 13-16 November 2023

## Slide 8: Dust on Baffles
Source: A. Moscatello at 2nd ET annual meeting, Orsay, 13-16 November 2023

## Slide 9: Contribution to ET’s cost and logistics:
Largest UHV system in the world:
  1m diameter pipes, length 120 km
  Volume: 9.4 × 104 m3
  Surface area: 3.8 × 105 m2
Total cost assuming scaling from Virgo:
  560 M€ (1/3rd of construction cost)
Assuming Virgo approach:
13000 tons of raw steel
8000 modules 15 m long
8 modules/day production (includes leak and extensive quality control checks)
240 pumping stations every 500m (5000 l/s effective, ionic, getter, auxiliary turbo molecular)
720 gate valves (250 mm)
48/72 gate valves (1 m diameter)
10 ovens (each 4 modules at times) operating ~3 years 24/7 for air-firing
4 cleaning systems
Bakeout (2G heat dissipation is ≈ 250 W/m @ 150°C )
Lots of time and cost saving possible on several of these items:
Material type: various steel species with varying price
Amount of material: thickness & weight
Length of sections: produced off or on site?
Types of pumps: varying capacity
Less valves: but high risk for leaks
Avoid heat treatment and bakeout: ferritic steel vs stainless

## Slide 10: Different designs in 2nd gen interferometers:
From: A. Grado et al J. Vac. Sci. Technol. B 41, 024201 (2023)
All stainless steel
Thick walls require
no stiffeners
Thin walls require
corrugation
Very low cost
Large Energy cost
& Logistics!

## Slide 11: Concerted effort between ET and CERN
DESIGN
(Mechanical stability, supports, etc.)
MATERIAL
(Welding, manufacturing, cleaning, etc.)
VACUUM
(Layout, pumps, gauges, bake-out, etc.)
Studies
PRODUCTION
MEASUREMENT
Pre-prototyping
Pilot sector
FABRICATION
& TEST
Solution 1
FABRICATION
& TEST
Solution 2
FABRICATION
& TEST
Solution n
Source: C. Scarcia at 2nd ET annual meeting, Orsay, 13-16 November 2023

## Slide 12: Beampipe structural materials
Cosmic Explorer
Einstein Telescope
Austenitic stainless steel
(304L)
Mechanical properties
Formability and weldability
Corrosion resistance
(native)
Vacuum performance
(requires HT heat treatment)
Cost
(raw material)
Non ferromagnetic
(µR ≈ 1)
Ferritic stainless steel
Mechanical properties
Formability and weldability
Corrosion resistance
(native)
Vacuum performance
(native)
Cost
(raw material, 30-50% less than austenitic)
Ferromagnetic
(µR > 200)
Mild steel
Mechanical
properties
Formability and weldability
Corrosion resistance
(requires treatment)
Vacuum performance
(native)
Cost
(raw material, 80-85% less than austenitic)
Ferromagnetic
(µR ≈ 100- 200)
Source: C. Scarcia at XIII ET Symposium, Cagliari, 8-12 May 2023

## Slide 13: Material/vacuum
Reliable and predictable outgassing rate measured with a dedicated test bench.
Ø 400 mm x 2100 mm.
Thickness < 2 mm.
Corrugated solution.
Pumping speeds scaled to ET dimensions.
Materials:
  AISI 304L vacuum-fired [austenitic SS]
  S315MC [mild steel]
  AISI 441 [ferritic SS]
Objectives:
Verify water outgassing modelling.
Ultimate pressure after 80°C and 150°C bake-out.
Estimate outgassing rate of materials.
Source: C. Scarcia at 2nd ET annual meeting, Orsay, 13-16 November 2023

## Slide 14: Material/vacuum
Experimental verification of beneficial effects of increased pumping speed during heating.
Water pressure calculated from mass 18 signal
The difference between the model and the experimental data is of 20%
Source: C. Scarcia at 2nd ET annual meeting, Orsay, 13-16 November 2023

## Slide 15: Outgassing rate vs temperature
qH2 ≈ 1.5×10-15
mbar l s-1 cm-2
Example:
304L-VF chamber
Hydrogen
Water-like
Instruments & gauges
Source: C. Scarcia at 2nd ET annual meeting, Orsay, 13-16 November 2023

## Slide 16: Design
Proved mechanical stability of a corrugated pipe.
For the pilot sector: Preparation of the technical specifications for a price inquiry following CERN’s purchasing rules.
  Corrugated pipe: Ø 1000 x 1.5 - 2 mm
  Smooth pipe: Ø 1000 x 3 - 4 mm
Contact with industry to evaluate the feasibility of a large-scale production of the corrugated solution.
Source: C. Scarcia at 2nd ET annual meeting, Orsay, 13-16 November 2023

## Slide 17: Welding
Welding of ferritic stainless steels:
conclusive and positive tests
Identification of the source of welding problem (grain coarsening, martensite precipitation, etc.)
  Selection of a ferritic SS with better weldability (AISI 441, industrial partner).
  Improved welding parameters (characterization w/ Univ. of Ghent).
  Improved manufacturing steps (cracking during corrugation solved).
  Test welding techniques other than TIG (laser CW v. Pulsed).
In preparation for the pilot sector:
Price inquiry for raw material (coils).
  (preliminary contacts w/ APERAM, Arvedi, AST)
TIG on AISI 444
TIG on AISI 441
Credit: UGhent
TIG on AISI 441
Credit: CERN
See also Alexey’s talk

## Slide 18: Automated Welding under vacuum
New ways to tackle productivity rate and welding quality.
FEF GmbH, RWTH Aachen, Werkhuizen Hengelhoef and APERAM collaborated for the preliminary design of a forming-welding machine:
Laser beam welding under movable vacuum (30 mbar)
Possibility to weld realistically up to 500 m long sections
Possibility to integrate continuous QC monitoring (ultrasonic or X-ray imaging)
Space between ET beampipes very limited.
New compact and customizable orbital welding tools integrating laser seam tracker and endoscopes.
In case of a repair during operation, use of light and compact orbital milling machine.
  → Minimum space required 40/50 cm between two stacked tubes (insulation included)
Credit: Arc Machines Inc.
New Interreg proposal submitted with UAntwerpen
RWTH Aachen, FEF, Werkhuizen Hengelhoef

## Slide 19: Outlook: CERN pilot sectors
Up to 4 tubes Ø 1 m x 50 m
Corrugated or VIRGO-like solution (stacked or adjacent)
Possibility to test different materials
Pumping speeds scaled to ET dimensions
The installation will serve to test:
Installation and alignment of supports and tubes.
Welding and assembly tools and methods.
Leak detection scenarios
Ultimate pressure and outgassing measurement after bake-out.
Preliminary schedule
Main deliverable: provide design report by end 2025
We are open for other experimental measurements:
Dust concentration and displacement inside the tube.
Installation and alignment of baffles inside the tube.
Vibration transfer function studies.

## Slide 20: General Planning
Design
Observations:
Design of pipe arm in the critical path.
Hold point to line up choices for the vacuum system and bakeout equipment.
As the corrugated beampipe cannot be fabricated in due time with the required UHV characteristics, it is kept only for design studies while seeking a valid industrial partner.
The VIRGO geometry beampipe made of 4-mm thick AISI 441 is now prioritized for the first test with the pilot sector.
The support system of the pilot sector will be compatible with beampipes of different geometries.
NEXT: A review on material and design of the beampipe for the pilot sector will be organized in the coming months with an international panel.

## Slide 21: Conclusions & Outlook
Lots of simulations on various effects:
  Residual gas and pumping scheme
  Light scattering and baffles
  Dust on baffles and free falling dust
  Many other: alignment, cleaning, installation, safety
  Completing requirements document
CERN activities currently focus on
  Material choices
  Pipe and support structure design
  Acquisition of materials and services
  Planning the production of first pilot sector
  Production of preliminary TDR by end 2024
  Pilot sectors ready for testing by end 2025
Input from Flanders
  UGent: Materials, procurement, manufacturing (see Alexey’s talk)
  UAntwerpen: Support on pilot sector design and installation New hiring completed: P. Revathi will join CERN team as of Jan 2024